## Slide 1: Environmental Benefits of Automobile Recycling

## Slide 2
Glass
Steel & Iron
Aluminum, Zinc,
Copper
Rubber
Plastic
Dismantling
Metal Separation
Separation Residue
Treatment
Pre-Treatment
Waste Stream
Automobile Recycling
Zero Landfill Goal
Notes: <number>

## Slide 3: Vehicle Recycling Process
End-of-life Vehicle (10-12 million/yr)
Automobile Dismantler
Reusable Parts
-Engines
-Transmissions
-Doors
-Bumpers
Recycle Fluids
Engine oil
Coolant
Refrigerant
Gasoline
Recycle Materials
Battery
Catalytic converter
Tires
Plastics (bumpers)
Automobile Shredder
Auto
Shredder
Residue
Approximately
18% by weight
Landfill
ASR is approximately
1.5% of material
sent to landfill
(by volume)
Ferrous Metals
Approximately 72%
Of vehicle by weight
Nonferrous metals
Approximately 3%
Of vehicle by weight
New Products
-New vehicles
-Vehicle components
-Building construction
ASR is composed of:
Plastics – 38%
Rubber – 21%
Glass – 12%
Fluids – 12%
Other – 15%
(paper, foam, fabric)
In most states ASR is
non-hazardous landfill
material and may be
used as landfill day
cover to control erosion,
leaching, pests, etc.
Remanufacturered
Parts
-Starters
-Alternators
-Water pumps
-Clutches
-Condensors
Existing Vehicle
New Vehicle
A variety of recycled material may also be used in new vehicle production such as:
lead from old batteries, plastics from consumer products, rubber from old tires,
windshields from industrial glass scrap, sound deadening material from carpet.
Car Recycling Steps: 1. Pretreatment 2. Dismantling 3. Metal Separation 4. Landfill disposal
1
2
3
4
Other New Products

## Slide 4
Vehicle Pretreatment
Fuel
Engine oil
Antifreeze
Wiper fluid
Transmission oil Brake fluid
Power steering oil Refrigerant
Batteries
Tires
Airbags
Mercury switches

## Slide 5: Fluid Recovery Calculation
1. RECOVERY INDEX - Percent of vehicles with fluids collected from reservoirs.
  Gasoline – 90 %
  Engine Oil – 95 %
  Transmission Oil – 95 %
  Steering and Brake Fluid – 95%
  Coolant – 90 %
  Refrigerant (Self Serve) – 25 %
  Refrigerant (Full Serve) – 72 %
  Wiper Fluid - 90%
2. FLUID SYSTEM QUANTITY - Average quantity per vehicle in gallons (in kg).
  Gasoline – 5.0 gal (14.22 kg)
  Engine, Transmission, Steering and Brake Oil – 2.02 gal (6.5 kg)
  Coolant – 0.9 gal (3.6 kg)
  Wiper Fluid – .5 gal (1.8kg)
  Refrigerant – 1.3lbs (.6 kg)

## Slide 7
Metal | GHG reductions per Ton | Tons of Recycled Material | GHG Reductions
 |  | An Example figure. | 
Recycled Steel | 0.86 | 100,000 | 86,000
Recycled Aluminum | 9.87 | 50,000 | 493,500
Recycled Copper | 3.52 | 30,000 | 105,600
 | Total GHG Reductions (Tons) |  | 685,100
Green House Reductions

## Slide 8: Environmental Benefits of Recycling
Energy Saved
Green House Gas Reductions
Water Conserved
Landfill Diverted
Air Emissions Reductions
Natural Resources Saved

## Slide 9: Aluminum Recycling Benefits
When Recyclers separates and collect aluminum parts for recycling it reduces the energy required for making new aluminum parts and the CO2 emissions by 95%.
Aluminum parts made from recycled material also reduces air pollution by 95%
Generation of landfill waste and use of water is also reduced by recycling aluminum
Aluminum can be recycled and reused indefinitely without a decline in material performance or quality

## Slide 10: Steel Recycling Benefits
Recyclers prepare vehicles for treatment by scrap metal processors to separate and recycle large quantities of iron and steel.
Using recycled steel saves 74% of the energy opposed to producing it from raw material
Every pound of steel recycled saves 5,450 BTUs of energy
Every ton of recycled steel saves 2,500 pounds of iron ore, 1,000 of coal, and 40 pounds of limestone.

## Slide 11: Metal Recycling Benefits
Recycling metal prevents the need to mine additional raw materials, the primary ingredients to make new metal.
Producing new metal from virgin materials requires more non-renewable energy than metal made from recycled material.
Metal recycling saves landfill space as well as provides a scrap resource to the metal industry.
Metal is a sustainable material and can be recycled over and over again.